Design

24core Singlemode Optical Fiber Loose Tube Cable      with Steel Wire Armored Communication Fiber Optic Cable Outdoor Communication Cable (GYXTSS)

Technical data

| No. of cable |  | 24 |
| --- | --- | --- |
| Fiber Model |  | G.652D |
| Strength Member | Material | Steel Wire |
|  | Diameter（±0.05）mm | 2.5mm |
|  | NO | 24core |
| Loose Tube | Material | PBT |
|  | Diameter（±0.06）mm | 1.8 |
|  | Thickness（±0.05）mm | 0.28 |
| Water Blocking layer（Material） |  | Cable Filling Compound |
| Armoring | Material | Steel Wire |
|  | Thickness（±0.05）mm | 0.95 |
| Outer Sheath | Material | HDPE |
|  | Thickness（±0.1）mm | 1.5 |
|  | Color | Black |
| Cable Diameter（±1）mm |  | 19 |
| Cable Weight（±5）kg/km |  | 73 |
| Min. bending radius | Without Tension | 10.5×Cable-φ |
|  | Under Maximum Tension | 20.0×Cable-φ |
| Temperature range （℃） | Installation | -20~+60 |
|  | Transport &Storage | -40~+70 |
|  | Operation | -40~+70 |

Fiber Colors

| No. | 1 | 2 | 3 | 4 | 5 | 6 |
| --- | --- | --- | --- | --- | --- | --- |
| Color | Blue | Orange | Green | Brown | Grey | White |

The properties of single mode optical fiber (ITU-T Rec. G652D)

| Item | Specification |
| --- | --- |
| Fiber type | Single mode |
| Fiber material | Doped silica |
| Attenuation coefficient @ 1310 nm @ 1383 nm @ 1550 nm @ 1625 nm | 0.35 dB/km 0.30 dB/km 0.21 dB/km 0.24 dB/km |
| Point discontinuity |  0.05 dB |
| Cable cut-off wavelength |  1260 nm |
| Zero-dispersion wavelength | 1300 ~ 1324 nm |
| Zero-dispersion slope |  0.092 ps/(nm2.km) |
| Chromatic dispersion @ 1288 ~ 1339 nm @ 1271 ~ 1360 nm @ 1550 nm @ 1625 nm | 3.5 ps/(nm. km) 5.3 ps/(nm. km) 18 ps/(nm. km) 22 ps/(nm. km) |
| PMDQ (Quadrature average*) | 0.2 ps/km1/2 |
| Mode field diameter @ 1310 nm | 9.2±0.4 um |
| Core / Clad concentricity error |  0.5 um |
| Cladding diameter | 125.0  0.7 um |
| Cladding non-circularity | 1.0% |
| Primary coating diameter | 245  10 um |
| Proof test level | 100 kpsi (=0.69 Gpa), 1% |
| Temperature dependence 0oC~ +70oC @ 1310 & 1550nm |  0.1 dB/km |

Main mechanical & environmental performance test

| Item | Test Method | Acceptance Condition |
| --- | --- | --- |
| Tensile Strength IEC 794-1-2-E1 | - Load: Short term tension - Length of cable: about 50m | - Fiber strain  0.33% - Loss change  0.1 dB @1550 nm - No fiber break and no sheath damage. |
| Crush Test IEC 60794-1-2-E3 | - Load: Short term crush - Load time: 1min | - Loss change  0.05dB@1550nm - No fiber break and no sheath damage. |
| Impact Test IEC 60794-1-2-E4 | - Points of impact: 3 - Times of per point: 1 - Impact energy: 5J | - Loss change  0.1dB@1550nm - No fiber break and no sheath damage. |
| Temperature Cycling Test YD/T901-2001-4.4.4 .1 | - Temperature step: +20oC→-40oC→+70oC →+20oC - Time per each step: 12 hrs - Number of cycle: 2 | - Loss change  0.05 dB/km@1550 nm - No fiber break and no sheath damage. |